## Slide 1: USE OF FLY ASH IN DIFFERENT COUNTRIES
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Notes: NUCLEAR POWER CORPORATION OF INDIA LIMITED

## Slide 2
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Various areas of use of Ash

## Slide 3
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Ash production and use in different countries
Country/Region | Ash Production (Million ton) | Ash Utilization (Mt) | Utilization Rate % | Year | References
USA | 134.7 | 55.6 | 42.0 | 2008 | ACAA, 2009
China | 120.02 | 69.6 | 58.0 | 2000 | Wang, 2004
EU 15 | 56.4 | 52.4 | 92.9 | 2008 | ECOBA, 2009
Australia | 13.8 | 2.5 | 18.0 | 2008 | ADAA. 2009
Japan | 11.0 | 10.7 | 97.2 | 2006 | JCOAL, 2010
Canada | 6.6 | 2.3 | 33.0 | 2006 | CIRCA, 2010
India | 145 | 78 | 50 | 2009 | FAU

## Slide 4
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Utilization of Ash in USA; Different avenues (based on ACAA, 2009)
Production 134.7 Million Ton
Utilization 55.6 (42%)
Disposal 79.06

## Slide 5
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
CCP Categories | Fly Ash | Bottom Ash | Boiler Slag | FGD | Total
1. Concrete/Concrete Products /Grout | 9.80 | 0.56 | - | 0.24 | 10.59
2. Blended Cement/ Raw Feed for Clinker | 2.44 | 0.72 | - | 0.42 | 3.58
3. Flowable Fill | 0.26 | 0.11 | - | 0.04 | 0.41
4. Structural Fills/Embankments | 4.65 | 2.94 | 0.06 | 1.36 | 9.02
5. Road Base/Sub-base | 0.20 | 0.77 | - | - | 0.97
6. Soil Modification/Stabilization | 0.67 | 0.19 | - | 0.10 | 0.96
7. Mineral Filler in Asphalt | - | - | 0.05 | - | 0.05
8. Snow and Ice Control | - | 0.48 | - | 0.05 | 0.53
9. Blasting Grit/Roofing Granules | 0.05 | 0.08 | 1.62 | - | 1.74
10. Mining Applications | 2.15 | 0.50 | 0.04 | 12.31 | 15.00
11. Gypsum Panel Products | - | - | - | 7.29 | 7.29
12. Waste Stabilization/Solidification | 3.52 | 0.01 | - | 0.22 | 3.74
13. Agriculture | 0.10 | - | - | 0.28 | 0.39
14. Aggregate | 0.09 | 0.45 | 0.03 | - | 0.57
15. Miscellaneous/Other | 0.80 | 0.47 | 0.03 | - | 1.30
Total Utilization |  |  |  |  | 55.6
Disposal |  |  |  |  | 79.06
Cont…

## Slide 6
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Utilization of Ash in Europe (EU15); Different avenues (based on ECOBA, 2009)
Production 56.42 Million Ton
Utilization 54.8 (92.9%)
Disposal 4.00

## Slide 7
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Total Production | 56.42 Mt |  |  | 
Sector of use | Fly Ash | Bottom Ash | Boiler Slag | Other
Cement raw material | 3.863 | 0.311 |  | 
Blended cement | 2.46 | 0.064 |  | 0.005
Concrete addition | 5.76 | 0.065 | 0.13 | 
Aerated concrete blocks | 0.663 | 0.009 |  | 
Non-aerated concrete blocks | 0.311 | 0.886 |  | 0.049
Lightweight aggregate |  |  |  | 
Bricks + ceramics | 0.093 | 0.019 |  | 0.057
Grouting | 0.346 | 0.015 | 0.067 | 
Asphalt filler | 0.095 |  |  | 
Subgrade stabilisation | 0.128 | 0.161 |  | 0.01
Pavement base course | 0.003 | 0.122 | 0.412 | 
General engineering fill | 1.556 | 0.516 |  | 0.091
Cont…

## Slide 8
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Cont…
Structural fill | 1.841 | 0.182 |  | 0.019
Soil amendment | 0.04 |  |  | 0.002
Infill | 0.446 |  |  | 0.064
Blasting grit | 603 |  | 0.603 | 
Plant nutrition |  |  |  | 0.008
Set retarder for cement |  |  |  | 0.638
Projection plaster |  |  |  | 0.817
Plaster boards |  |  |  | 5.577
Gypsum blocks |  |  |  | 0.303
Self levelling floor screeds |  |  |  | 1.533
Other uses | 0.087 | 0.068 | 0.144 | 0.086
Reclamation, Restoration | 17.079 | 1.901 |  | 1.874
Temporary stockpile | 0.829 | 0.216 |  | 0.321
Disposal | 2.231 | 0.459 |  | 1.383

## Slide 9
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Utilization of Ash in Australia; Different avenues (based on ADAA, 2009)
Production 13.76 Million Ton
Utilization 2.51 (18.0%)
Disposal 11.25

## Slide 10
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Total Ash Produced | 13.76 | Mt |  | 
CCP Use (M Tonnes) | Fly Ash | Bottom Ash | Cenosphere | Combined
Category 1 |  |  |  | 
Concrete/Concrete Products /Grout | 1.55 | 0.02 | 0.00 | 1.57
Cement/ Raw Feed for Clinker |  |  |  | 
Mineral Fillers |  |  |  | 
Category 2 |  |  |  | 
Flowable Fill CLSM | 0.31 | 0.22 | 0.00 | 0.53
Structural Fills/Embankments |  |  |  | 
Road Base/Sub-base |  |  |  | 
Soil Modification/Stabilization |  |  |  | 
Mineral Filler in Asphalt |  |  |  | 
Agriculture |  |  |  | 
Aggregate |  |  |  | 
Category 3 |  |  |  | 
Mining Applications (e.g. Backfill) | 0.11 | 0.00 | 0.00 | 0.11
Waste Stabilization/Solidification |  |  |  | 
Miscellaneous/Other |  |  |  | 
Total of All Beneficially Used in 2008 | 0.03 | 0.26 | 0.01 | 2.22
Total of All Sold in 2008 | 1.97 | 0.24 | 0.00 | 0.29
Disposal |  |  |  | 11.25
Cont…

## Slide 11
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Utilization of Ash in Japan; Different avenues (based on JCOAL, 2006)

## Slide 12
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Item |  | Electric Power Utilities |  | General Industries |  | Total | 
Sector | Contents | Qty | % | Qty | % | Qty | %
Cement | Raw material | 4816 | 61.64 | 2069 | 72.75 | 6885 | 62.61
 | Admixture | 103 | 1.32 | 174 | 6.12 | 277 | 2.6
 | Ready mixed | 109 | 1.4 | 0 | 0 | 109 | 1.02
 | Total | 5028 | 64.35 | 2243 | 78.87 | 7271 | 66.23
Public works | Soil treatment | 209 | 2.68 | 102 | 3.59 | 311 | 2.92
 | Public works | 506 | 6.48 | 35 | 1.23 | 541 | 5.08
 | Public works for electric power | 46 | 0.59 | 0 | 0 | 46 | 0.43
 | Subgrade stabilization | 136 | 1.74 | 162 | 5.7 | 298 | 2.8
 | Asphalt filler | 10 | 0.13 | 0 | 0 | 10 | 0.09
 | Backfilling in coal mines | 203 | 2.6 | 0 | 0 | 203 | 1.9
 | Total | 1110 | 14.21 | 299 | 10.51 | 1409 | 13.22
Cont…

## Slide 13
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Construction works | Construction board | 227 | 2.91 | 138 | 4.85 | 365 | 3.42
 | Lightweight aggregate | 0 | 0 | 0 | 0 | 0 | 0
 | Concrete product | 29 | 0.37 | 1 | 0.04 | 30 | 0.28
 | Others | 0 | 0 | 0 | 0 | 0 | 0
 | Total | 256 | 3.28 | 139 | 4.89 | 395 | 3.71
Agriculture, forestry & fisheries | Fertilizer | 50 | 0.64 | 22 | 0.77 | 72 | 0.68
 | Soil improvement | 10 | 0.13 | 79 | 2.78 | 89 | 0.64
 | Thawing material | 0 | 0 | 0 | 0 | 0 | 0
 | Total | 60 | 0.77 | 101 | 3.55 | 161 | 1.31
Others | Sewage | 2 | 0.03 | 1 | 0.04 | 3 | 0.03
 | Iron manufacture | 11 | 0.14 | 1 | 0.04 | 12 | 0.11
 | Others | 1346 | 17.23 | 60 | 2.11 | 1406 | 13.19
 | Total | 1359 | 17.39 | 62 | 2.18 | 1421 | 13.33
Disposal |  |  |  |  |  |  | 2.8
Cont…

## Slide 14
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Utilization of Ash in Canada; Different avenues (based on CIRCA, 2010)

## Slide 15
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Total Production | 6.4 | Mt |  |  | 
Uses Area | Fly Ash | Bottom Ash | FGD Gypsum | Other | Total
Cement | 0.638 | 0.147 | 0.01 | 0 | 0.795
Concrete / Grout | 0.472 | 0 | 0 | 0 | 0.472
Mining Application | 0.089 | 0 | 0 | 0 | 0.089
Road Base / Subbase | 0.017 | 0.094 | 0 | 0 | 0.111
Wall Board | 0 | 0 | 0.313 | 0 | 0.313
Other | 0.084 | 0.006 | 0.043 | 0.039 | 0.172
Disposal |  |  |  |  | 4.45
Cont…

## Slide 16
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Utilization of Ash in China; Different avenues (based on Wang & Wu, 2004)
Disposal 56,8%
Construction industries and Civil engineering 32,8%
Restoration 6,7%
Agriculture 1,8%
Others 1,9%
In some developed areas, Shanghai, Nanjing and Nantong of Jiangsu Province and Nanchang of Jiangxi Province, the utilization rate of produced fly ash was 100% in the past five years and used extensively in geotechnical engineering of road construction and wallboard materials

## Slide 17
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Fly ash in high value added applications
Category | High value-added applications
Mineral extraction | Alumina Magnetite Iron Carbon Cenospheres Other minor and trace items

## Slide 18
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Category | High value-added applications
Construction and engineering | Enhanced Pozzolana cement Oil Well Cement Decorative glass Ceramic Fibers Glazed floor and wall tiles Ash alloys Synthetic marble High ware resistance ceramic tile Reflective material Ultra light hollow sphere for arid zone Continuous casting mould powder Domestic cleaning powder Synthetic wood
Cont…

## Slide 19
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Cont…
Category | High value-added applications
Filler | Mineral fillers Distemper Plastic fillers
Protective material | Fire Bricks Fire abatement applications Glass Ceramics Foam insulation products Anti-corrosion coating Mineral Wool
Waste treatment material | FGD Adsorbent Synthetic Zeolites Activated Cenospheres
Agriculture | Cultivation Potassium silicate fertilizer

## Slide 20
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Cont…
These kinds of high value added products consume lower volume of fly ash than that of construction, back fill and road pavement applications
However, they have the potential in generating considerable sales revenues for power plants and manufacturers, which helps to prompt the development of different high level Ash technologies

## Slide 21
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Eco-Industry Park
(A conceptual model)
EIP derived from the idea of industry symbiosis could be realized to optimize and maximize the use of Ash
Ash generated from the power plants are used as feed stocks for various applications and the produced electricity is supplied to those plants as primary energy source

## Slide 22
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>

## Slide 23
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
There is a need for concerted effort to promote the "technically sound", "environmentally safe", and "economically justified" utilization of Ash.
A number of researches and projects on high levels utilization of Ash have been carried out in many part of world, however, the majority of which have not yet been commercialized.
It should be emphasized that transforming such laboratory- or pilot-scale technologies into industrial productivity is of the highest priority for increased use of Ash.
Conclusion

## Slide 24
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
Fly ash should be considered as an essential ingredient of concrete and not merely for replacement of cement or reduction in cost
Notes: NUCLEAR POWER CORPORATION OF INDIA LIMITED

## Slide 25
2/22/2011
USE OF FLY ASH IN DIFFERENT COUNTRIES
<number>
ThanQ?